## Slide 1
Raman study of the Flash-lamp annealing influence to Cu2ZnSnS4 nanocrystals and PEDOT:PSS composite thin films
Yevhenii Havryliuk1,2,3, Volodymyr Dzhagan3, Anatolii Karnauhov3, Oleksandr Selyshchev1,2, Dietrich R.T. Zahn1,2
1 Semiconductor Physics, Chemnitz University of Technology, Chemnitz, Germany
2 Center for Materials, Architectures, and Integration of Nanomembranes (MAIN), Chemnitz, Germany
3 V.E. Lashkaryov Institute of Semiconductor Physics NAS of Ukraine, Kyiv, Ukraine
Data from Wikipedia
Motivation
One of the current trends is thin-film photovoltaic (PV). To improve properties of thin-film PV devices as well as to combine PV and thermoelectric (TE) effects researchers look towards replacing Si as an absorber layer with alternative affordable and environment-friendly materials with much stronger light absorption, TE properties, and lower cost of production.
non-toxic and abundant constituents;
high absorption coefficient in the whole visible range (up to an order of magnitude higher than that of Si)
- possibility of "green" colloidal synthesis.
- multiple structural modifications; - secondary phases; - a lot of intrinsic defects.
Wan-Ching Hsu, et al., Science, 345, 542 (2014)
The increasing demand for energy as well as ecological issues enhances research in the areas of renewable sources.
Cu2ZnSnS4 nanocrystals (CZTS NCs) - perspective materials for renewable energy
Results & discussion
Advantages:
Issues:
Acknowledgment
Summary
- For the first time the Raman scattering spectra of CZTS NCs in PEDOT:PSS matrix with CZTS NCs concentration from 0% to 100% were obtained and analysed. It is shown that with varying concentration of CZTS NCs changes occur in both.
Picture from: https://utrecht.materialdistrict.com/thin-film-solar-cells/
Perspectives:
PV power conversion already reached 12,6%;
pronounced TE properties;
- new composites obtained by mixing CZTS NCs colloidal solution with conductive polymers;
- enhancing of PV and TE properties not only by (post-)synthesis treatment (e.g. different deposition methods and conditions, thermal or flash-lamp annealing of the films) but also by varying the stoichiometry.
CZTS NCs + PEDOT:PSS composite
Shifting of the characteristical modes of CZTS NCs and PEDOT:PSS in the composite compound compared to the pure materials confirms the interaction between these two materials.
12 J/cm2 FLA energy density was chosen as an optimal one from the previous results
Flash-lamp annealing
Almoust no influence on PEDOT:PSS
Even more improvement of crystalline quality of CZTS NCs in composite compound compared to pure CZTS NCs and complete decomposition of PEDOT:PSS
- For the first time the influence of the FLA treatment to the mixed CZTS NCs and PEDOT:PSS composite were investigated. The better improvement of CZTS NCs crystalline quality in composite observed due to PEDOT:PSS plays protective role.
S. Bourdais et al. Adv. Energy Mater. 1502276, 1 (2016)
The aqueos colloidal solution of CZTS NCs with average size of 5 - 10 nm obtained by us with „green“ synthesis mixed in different volume ratios of PEDOT:PSS, deposited to glass substrate and Raman spectra are taken
Shift of PEDOT:PSS peak in composite
Presence of TGA as a ligand and possible presence of small amount in NCs solution
Mixture of PEDOT:PSS with expected TGA amount and supernatant prepared
Similar behaviour of PEDOT:PSS main peak. No clear answer about the reason of the shift
Further detailed investigation of this question required
- The shift of PEDOT:PSS characteristic peak observed for mixing PEDOT:PSS with supernatant, highly diluted TGA and NaOH, what require further investigation.
Expected crystalline quality improvement for pure CZTS NCs
PEDOT:PSS plays protective role for CZTS NCs „hot spots“
PEDOT:PSS – very vell known conductive polymer
easy tunable electrical and thermoelectrical properties
poly(3,4-ethylenedioxythiophene) polystyrene sulfonate
can be used for thin-film transparent solar cells
improving of properties by adding nanoparticles